Design and synthesis of oxime esters as photoinitiators using quantum chemical calculations and machine learning

Yuya Watanabe, a Fuka Takahata, b Mahiko Utoguchi, b Takuya Sekizawa, b Haruka Nagano, b Shunichi Himori, b Akihiko Yamada, b and Hiroaki Gotoh *,a

aDepartment of Applied Chemistry, Yokohama National University, 79-5 Tokiwa-Dai, Hodogaya-Ku, Yokohama 240-8505, Japan

bAir Water Performance Chemical, Inc., Research & Development Center, 1-2 Chidori-Cho, Kawasaki-Ku, Kawasaki 210-0865, Japan

*Corresponding author. Email: gotoh-hiroaki-yw@ynu.ac.jp

Content

Attached File List	3

Machine Learning	9

Dense Neural Network	9

ABT-MPNN	9

GPT	10

Detail of Assembly Method	11

Evaluation functions in the Generative method	11

Symmetry Score	11

Fused Ring Count Score	11

Number of Aromatic Heterocycle Score	12

Max Ring Size Score	12

Oxime Activation Part Score	12

Oxime Ester Property Score	12

Generated Compounds’ quantum chemical calculation result	13

F-01	13

F-02	14

A-01	15

A-02	18

G-01	21

G-02	24

Synthetic Routes and NMR	26

F-01	26

F-02	27

A-01	27

A-02	28

G-01	29

G-02	29

NMR Spectrum	31

F-01	31

F-02	31

A-01	32

A-02	32

G-01	33

G-02	33

Attached File List

1. Training dataset for the oxime ester prediction model: all_SMILES.csv

Contains SMILES strings used for model training and testing, as well as the T1, S1, and S1 oscillator intensities.

2. Oxime ester dataset converted from Aldrich to Ketones: filter_SMILES.csv

Contains T1, S1, and S1 oscillator intensities predicted by the optimized ABT-MPNN prediction model.

3. Molecules generated by Assembly: Assembly_SMILES.csv

Lists T1, S1, and S1 oscillator intensities predicted by the optimized ABT-MPNN prediction model.

4. Oxime ester dataset generated by the generative model: generative_SMILES.csv

Contains T1, S1, and S1 oscillator intensities predicted by the optimized ABT-MPNN prediction model.

- Experimental

  - Dataset

Table S1 presents a detailed breakdown of the datasets used for creating the predictive models and implementing the Filter, Assembly, and Generative methods.

A total of 385 compounds, including commercial, known, and virtual (small-molecule) compounds were used to train the models for predicting the physicochemical indices. The commercial products were 200 oxime esters sourced from Aldrich reagents in PubChem (retrieved on 2022.10.11).19 The known compounds were 134 oxime esters synthesized and reported in 19 studies.1,3,4,11–13,15–18,20–28 These compounds were retrieved through a literature search. The virtual molecules were 51 small oxime esters with a broad range of light absorption. Additional details are provided in the ESI (all_SMILES.csv).

For the Filter method, we designed ready-to-use oxime esters that could be synthesized from commercially available ketones. The commercial dataset included 251,394 compounds from Aldrich. Ketones were extracted and converted into oxime esters following the procedure described in Section 2.3.4, resulting in 1293 oxime esters.

The dataset used for the Assembly method was the same as the dataset of 385 oxime esters used in the prediction model described in Section 2.3.

In the Generative approach, commercially available compounds were used for pretraining, and a dataset of known oxime esters was used for finetuning. Specifically, the Aldrich dataset (25,1394 compounds) was used for pretraining, whereas 64 oxime esters were used for finetuning, as described in Section 2.3.6.

Table S1 Dataset composition

| Method | Compound Group | Composition | Total |
| --- | --- | --- | --- |
| Filter | Ketone | Aldricha) (1293) | 1293 |
| Assembly | Oxime Ester | Aldricha) (200), Literature reviewb) (134), Virtual moleculesc) (51) | 385 |
| Generative (Pretrained) | General | Aldricha) (251,394) | 251,394 |
| Generative (Finetuned) | Oxime Ester | After hierarchical clustering Oxime estersb,d) (64) | 64 |

a) retrieved from PubChem; b) derived from 19 reports through a literature search; c) molecules exhibiting low-wavelength light absorption; d) oxime esters categorized by hierarchical clustering: the oxime ester dataset from b) was categorized using hierarchical clustering based on a Levenshtein distance matrix constructed for Simplified Molecular Input Line Entry System (SMILES) strings

  - Quantum Chemical Calculation

Quantum chemical calculations were performed to calculate physicochemical indices for the 385 molecules used in the Assembly method. Gaussian 1629 software was used for these calculations: First, 10,000 initial conformations were generated using RDKit’s30 ETKDG31 method. Structural optimizations were performed in the Merck molecular force field (MMFF94).32 The most stable conformation was further optimized using PM6 and B3LYP /6-31G(d) computations, followed by vibrational analysis and single-point energy calculations for excited states using B3LYP /6-31G(d). From these calculations, T1 energy, S1 energy, and oscillator strength of the compounds were obtained. For compounds to be synthesized, the same process was followed, with final single-point energy calculations conducted using cam-B3LYP/6-31G(3d2f, 2d2g) to determine the physicochemical indices.

  - Machine Learning

Quantum chemical calculations of the 385 oxime esters were used to train the predictive models. The prediction models included a fully connected neural network33, a graph-based neural network (atom-bond transformer-based message passing neural network, ABT-MPNN34), and a GPT-based neural network35. The objective variables were T1 energy, S1 energy, and oscillator intensity. The oscillator intensity was log-transformed, as numerous molecules exhibited vibrational intensities ranging from 10-2 to 10-4:

| y= -log10(x + 10-8) |  |
| --- | --- |

where x and y denote the oscillator intensities before and after the transformation, respectively.

Cross-validation was performed for model validation. The dataset was randomly divided into five parts, with 80% used for training and 20% for testing. To compare models under the same conditions, the same split data were used for each training session, using the mean squared error function for evaluation.

    - Fully Connected Neural Network

This model was implemented in Pytorch36 (ver. 2.0.0), training Morgan Fingerprints37 (nBits = 2048, radius = 3) as descriptors. The model involved 13 layers, with a learning rate of 1×10-5.

    - Graph-based Neural Network

ABT-MPNN served as the graph-based neural network, trained with five layers at a rate of 1×10-5. The descriptors included the adjacency, distance, and Coulomb matrices. Bonding information between intramolecular atoms (conjugation system, bond order, etc.) and intramolecular atomic features (atomic number, aromaticity, etc.) were calculated using RDKit. L1 loss was used as the loss function.

    - GPT-based Neural Network

This model was established to make predictions from SMILES strings, based on the generative pretrained transformer (GPT) used in natural language processing. As the output layer of the typical GPT model is a SoftMax function, we replaced the output layer with a linear layer to apply it to the regression task.

    - Filter Method

A total of 1293 ketones were obtained by extracting molecules with molecular weights exceeding 50, aromatic rings, and one ketone skeleton from Aldrich’s commercially available drug data set (251,394 ketones). Ketone to oxime ester conversion was performed using the RDKit library. The process involved identifying the ketone moiety in the molecule and converting the ketone to the oxime ester structure. From the 1293 datapoints, the prediction model described in Section 2.3 was used to extract compounds with S1 energy < 3.5 eV, T1 energy > 2.7 eV, and S1 oscillator intensity > 1.0.

    - Assembly Method

The 385 molecules in the dataset described in Section 2.1 were split into side chains and main skeletons using the MurckoScaffold function in RDKit. These components were shuffled. Gasteiger charges38 of the aromatic atoms of the main frame containing aromatic rings were calculated, and the molecule was designed by introducing side chains containing oxime esters at the positions of aromatic atoms with low Gasteiger charges. This approach resulted in a molecular structure containing one to three oxime ester active sites.

    - Generative Model

Transformer-based language models and Taiga39 with reinforcement learning were used as generative models. To train the model on SMILES40 strings, pretraining was performed on the Aldrich (25,294) dataset. The dataset of 385 oxime esters was used to create a Levenshtein distance matrix41,42 for SMILES strings. Hierarchical clustering (AgglomerativeClustering) using Scikit-Learn42 was applied to group 64 oxime esters. This clustering was required to address the presence of several pairs of similar SMILES strings in the dataset, which could hinder the generation of diverse SMILES strings. Reinforcement learning was conducted to optimize the physical properties. The rewards functions included the following: 1) Symmetry score: molecular symmetry); 2) Fused ring count score: Number of rings in the fused ring containing the most alkyl rings in the molecule; 3) Num aromatic heterocycle score: Number of aromatic heterocycle rings; 4) Molecular weight score; 5) Number of oxime ester prop score: Number of oxime ester parts; and 6) Oxime ester prop score. Table S2 lists the target values for these rewards functions. Details of the evaluation functions can be found in the ESI.

The generated SMILES outputs were characterized by molecular weights between 300 and 600, structural similarity (based on the standardized Levenshtein distance) of less than 0.7 with the training data, and reasonable SMILES structures.

Table S2 Reward functions for reinforcement learning

| Physical property | Target |
| --- | --- |
| Symmetry | 0.6 |
| Fused ring count | 3 |
| Number of aromatic heterocycles | 3 |
| Maximum ring size | 5, 6 |
| Number of oxime parts | 3 |
| Oxime ester property | 2.5 |

  - Synthesis of Oxime Esters

The oxime esters generated using the Filter, Assembly, and Generative methods were synthesized following the route shown in Figure S1. First, Friedel–Crafts acylation was performed to convert the chromophore to a ketone. Subsequently, the ketone body was converted to ketoxime through ketoximation. The ketoxime was reacted with an alkyl chloride to obtain the oxime ester. If chromophore synthesis was required, it was performed using known protcols.4 The synthesized oxime esters were identified through proton nuclear magnetic resonance (1H-NMR; ECA 500, 500 MHz). Details of the synthetic route can be found in the ESI. UV–visible (UV–Vis) absorption spectra of the oxime esters were measured at 300–800 nm in acetonitrile solvent.

Figure S1 Relation between predicted oxime ester scores and quantum calculated oxime ester scores. Each physicochemical indices (T1, S1, oscillator strength at S1) were predicted by using ABT-MPNN model. Quantum chemical calculation exec with B3LYP/6-31G(d) condition.

Scheme S1 Synthetic route of oxime ester

Figure S2 UV–Vis spectra of synthesized oxime esters, measured in acetonitrile solvent. Left axis shows the molar extinction coefficient, and right axis shows the oscillator strength computed by quantum chemical calculations (cam-B3Lyp 6-31G(3d2f, 2d2p)).

  - Measurements

The polymerization performance, in terms of heat flow and monomer conversion, of the synthesized oxime esters and comparative molecule OXE01 (BASF) was assessed through photo-differential scanning calorimetry (Photo-DSC; XDSC-7000, Hitachi High-Tech, Japan).43,44 Trimethylolpropane triacrylate (TMPTA) (Tokyo Kasei Kogyo) was used as the monomer. Samples (0.5 or 1.0 mg, corresponding to 0.5–1.0 wt% photoinitiator in TMPTA) were analysed under a nitrogen atmosphere, with measurements obtained at a film thickness of ~500 μm, a wavelength of 405 nm (Hg lamp, h-line), and an intensity of 50 mW cm-2. The measurement was commenced 30 s before the start of irradiation and lasted for 0.5–5.5 min. The conversion of vinyl groups (C, %) was determined as

C = 100% × ∆Ht/∆HMtheory				(1)

where ΔHt is the heat release at time t, obtained by exothermic peak integration; and ΔHMtheory is the theoretical heat release for complete conversion. As TMPTA has three acrylate residues, ΔHMtheory was calculated as

∆HMtheory=3×∆HPtheoryMm= 797.71 mJ mg-1 			(2)

where Mm is the molecular weight of TMPTA, and ΔHPtheory = 78.2 kJ mol-1 is the theoretical heating value.47

Machine Learning

We modeled and made predictions for S1, S1 oscillator intensity, and T1, with DenseNeutralNetowrk and ABT-MPNN performing well with R2 greater than 0.7 for all indices (Figure S3).

Figure S3 Training results: The x- and y-axes represent the predicted values and values derived through quantum chemical calculations. Each model was evaluated using test data. Dense: fully connected neural network, ABT-MPNN: atom-bond transformer-based message passing neural network.

.

Dense Neural Network

The results of training evaluation by cross-validation are shown in Figure S4. Some results showed that R2 was lower than 0.6. However, many results show high prediction performance, which can be evaluated as good learning.

Figure S4 Training results of dense neural network

ABT-MPNN

The results of training evaluation by cross-validation are shown in Figure S5. Some results showed that R2 was lower than 0.6. However, many results show high prediction performance, which can be evaluated as good learning.

Figure S5 Training results of ABT-MPNN

GPT

The results of training evaluation by cross-validation are shown in Figure S6. In all results, R2 was less than 0.6, a poor prediction. This is consistent with the SMILES-based approach having several inherent limitations. The representational constraints of SMILES, which captures only 2D molecular structure while omitting crucial 3D stereochemical information, likely contributed to the model's inability to accurately predict properties that depend on spatial arrangements. Additionally, the complexity of the target properties, which are influenced by multiple factors beyond what can be encoded in simple SMILES strings, presents a fundamental challenge to the prediction task.

The model's performance may have also been impacted by data quality issues. Our training dataset, while extensive, likely contained imbalances in the representation of certain structural features and functional groups, leading to biased predictions particularly for compounds containing rare molecular frameworks. The applicability domain of our model is necessarily limited to chemical space similar to that covered in the training set, which explains the particularly poor performance on novel scaffolds.

Furthermore, the black-box nature of our deep learning approach makes it difficult to interpret which molecular features were driving the predictions, hindering our ability to systematically improve the model. The single-point predictions also fail to adequately convey prediction uncertainty, which would be valuable information for practical applications of the model.

Future work should explore alternative molecular representations that better capture 3D information, implement uncertainty quantification methods, and develop more interpretable models to overcome these limitations.

Figure S6 Training results of GPT model.

Descriptors for ABT-MPNN

The inputs to the ABT-MPNN include the interatomic feature matrix, bond feature matrix, adjacency matrix, Coulomb matrix, and molecular descriptors.

Inter-atomic feature matrix

This matrix represents a feature vector of physical and chemical properties of atoms within each molecule. The inputs include atomic number, formal charge, and atomic chirality.

Bond feature matrix

This matrix encodes intramolecular bonding information, including the type of bond, conjugation, and whether the bond is part of a ring structure.

Adjacency matrix

This matrix represents the connection information of atoms, indicating which atoms in the molecule are bonded to each other.

Distance matrix

This matrix indicates the spatial distances between atoms, calculated from the RDKit-generated conformers.

Coulomb Matrix

The Coulomb matrix describes the electrostatic interactions between atoms in a molecule.

Molecular Descriptor

These descriptors describe the characteristics of the molecule as a whole. In this study, molecular descriptors generated using RDKit were employed.

Detail of Assembly Method

The molecule was split into side chains and the main backbone using the MurckoScaffold function. The split side chains and main skeleton were shuffled. The Gasteiger charges38 of the aromatic atoms of the main frame containing aromatic rings were calculated, and the molecule was designed by introducing side chains containing oxime esters at the positions of aromatic atoms with low Gasteiger charges. This resulted in a molecular structure containing 1–3 oxime ester active sites.

https://github.com/poclab-web/DesignOximeEster/tree/main/oxime_ester_assembling

Evaluation functions in the Generative method

Symmetry Score

The Symmetry Score assigns canonical ranks to all atoms in a given molecule and counts the number of occurrences of each rank. Using this information, the total number of equivalent atom pairs is calculated, which is then normalized by the number of all atom pairs in the molecule to calculate the Symmetry Score. The Symmetry Score takes values between 0 and 1, with values approaching 1 indicating higher 2-dimensional symmetry of the molecule.

The reward function based on the Symmetry Score, SR, is shown below. SS is the molecule for which the aforementioned symmetry score (m) is input.

| SRm= SSm if SSm>0.6SRm=0 ≤0.6 |  |
| --- | --- |

The Symmetry Score is introduced because molecules with higher symmetry are more likely to contain multiple active sites. Specifically, a higher symmetry of the chromophore indicates a higher ease for performing Friedel-Crafts acylation over multiple sites.

Fused Ring Count Score

This score indicates the number of fused rings in a molecule and determines the number of alkyl rings within the largest fused ring. The reward function, FR, is defined as follows, where FS is the fused ring count score, and m is the input molecule.

| FRm=FSm if FSm>2 FRm=0 if FSm≤2 |  |
| --- | --- |

A larger fused ring has a higher potential to host multiple active sites; therefore, they are prioritized.

Number of Aromatic Heterocycle Score

This score indicates the number of aromatic heterocycles in the molecule. The reward function NR is defined as follows, where NS is the Num Aromatic Heterocycle Score, and m is the input molecule.

| NRm=NSm if NSm>2 NRm=0 if NSm≤2 |  |
| --- | --- |

Max Ring Size Score

This score indicates the largest ring size in the molecule. The reward function MR is set as follows, where MS is the Max Ring Size Score, and m is the input molecule.

| MRm=MSm if MSm=5 or 6 MRm=0 if MSm≠5 or 6 |  |
| --- | --- |

This constraint prevents the model from designing excessively large cyclic alkyl structures.

Oxime Activation Part Score

This score indicates the number of active sites of oxime esters. The reward function NOR is defined as follows, where

m is the molecule, and NO is the number of oxime ester active sites.

| NORm=NO(m) |  |
| --- | --- |

Oxime Ester Property Score

This score evaluates the oxime ester physical properties for a given molecule: first excited triplet energy ( T1 energy), first excited singlet energy (S1 energy), and S1 oscillator strength. As quantum chemical calculations of these values for each individual product molecule would be computationally expensive, the ABT-MPNN model is used to predict these values.

The reward function, OR, is set as follows, where ABTMPNNT1 is the T1 energy output by ABTMPNN, ABTMPNNS1 is the S1 energy output by ABTMPNN, and ABTMPNNS1osc is the S1 oscillator strength output by ABTMPNN. Although the model simultaneously outputs these values, they are represented as separate terms for notational convenience. Specifically, these functions do not exist independently and are strictly one function.

| ORm=ABTMPNNT1m[eV]+ABTMPNNS1m[eV]+ABTMPNNS1osc(m) |  |
| --- | --- |

Generated Compounds’ quantum chemical calculation result

F-01

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0       -6.126015   -2.404352    0.207614
      2          6           0       -5.428195   -1.099045   -0.103270
      3          8           0       -5.934529   -0.109756   -0.558116
      4          8           0       -4.094813   -1.231162    0.225828
      5          7           0       -3.346640   -0.054267   -0.016471
      6          6           0       -2.102904   -0.207180    0.280519
      7          6           0       -1.480778   -1.470623    0.820204
      8          6           0       -1.251294    0.994364    0.052401
      9          6           0       -1.805480    2.178450   -0.471249
     10          6           0       -1.000536    3.291377   -0.679249
     11          6           0        0.366022    3.250726   -0.387944
     12          6           0        0.925344    2.083824    0.140621
     13         16           0        2.663355    2.114232    0.590206
     14          6           0        3.222158    0.453699    0.203619
     15          6           0        3.105841   -0.081100   -1.088173
     16          6           0        3.605018   -1.349925   -1.365280
     17          6           0        4.256271   -2.109883   -0.380147
     18          6           0        4.822610   -3.471934   -0.705730
     19          6           0        4.375836   -1.559640    0.899914
     20          6           0        3.858513   -0.296528    1.197186
     21          6           0        0.113965    0.964857    0.366602
     22          1           0       -5.668841   -3.225293   -0.354469
     23          1           0       -6.032222   -2.641757    1.272483
     24          1           0       -7.179538   -2.315106   -0.059120
     25          1           0       -0.663276   -1.801067    0.169865
     26          1           0       -2.216138   -2.269141    0.896401
     27          1           0       -1.053415   -1.290208    1.813363
     28          1           0       -2.862332    2.204625   -0.710018
     29          1           0       -1.433710    4.199709   -1.089174
     30          1           0        0.994658    4.116112   -0.577108
     31          1           0        2.620790    0.496384   -1.869402
     32          1           0        3.500718   -1.753933   -2.370122
     33          1           0        5.713096   -3.390197   -1.342567
     34          1           0        4.096887   -4.089809   -1.247429
     35          1           0        5.114530   -4.011455    0.200683
     36          1           0        4.869841   -2.129323    1.683687
     37          1           0        3.945358    0.105531    2.202304
     38          1           0        0.562880    0.071921    0.785107
 ---------------------------------------------------------------------

F-02

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0        5.621446   -0.632521    0.029880
      2          6           0        4.155532   -1.005125    0.050489
      3          8           0        3.703125   -2.116882    0.094416
      4          8           0        3.412359    0.155441    0.008873
      5          7           0        2.015785   -0.079628    0.053904
      6          6           0        1.344094    1.014758   -0.049414
      7          6           0        1.939301    2.393695   -0.193584
      8          6           0       -0.136299    0.855328   -0.016247
      9          6           0       -0.985150    1.995146    0.078751
     10          6           0       -2.353374    1.858971    0.114691
     11          6           0       -2.965231    0.580334    0.054933
     12          6           0       -4.374007    0.402096    0.086524
     13          6           0       -4.924264   -0.858188    0.025061
     14          6           0       -4.090513   -2.001311   -0.071646
     15          6           0       -2.722481   -1.862263   -0.105218
     16          6           0       -2.120554   -0.574036   -0.042526
     17          6           0       -0.716944   -0.403580   -0.076036
     18          1           0        5.868384   -0.012212    0.897856
     19          1           0        6.219031   -1.544489    0.046213
     20          1           0        5.855763   -0.051146   -0.867881
     21          1           0        3.015880    2.342845   -0.345216
     22          1           0        1.744195    2.989534    0.706388
     23          1           0        1.482767    2.919881   -1.038569
     24          1           0       -0.553685    2.989131    0.130775
     25          1           0       -2.985353    2.740614    0.190920
     26          1           0       -5.011963    1.279752    0.160585
     27          1           0       -6.003499   -0.982629    0.050413
     28          1           0       -4.539247   -2.989731   -0.119101
     29          1           0       -2.078831   -2.735325   -0.178798
     30          1           0       -0.077141   -1.277123   -0.151170
 ---------------------------------------------------------------------

A-01

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0        9.780428   -7.052157    1.058548
      2          6           0        9.494313   -5.991744   -0.009558
      3          6           0        8.542807   -4.887717    0.470698
      4          6           0        8.254513   -3.829859   -0.603586
      5          6           0        7.403422   -2.640817   -0.124819
      6          6           0        5.995225   -2.981383    0.392278
      7          6           0        5.088542   -3.645398   -0.668497
      8          6           0        3.684503   -3.881430   -0.156525
      9          7           0        3.312253   -4.928193    0.499612
     10          8           0        4.390394   -5.840409    0.661293
     11          6           0        4.009324   -7.017362    1.267859
     12          6           0        5.231601   -7.894732    1.426538
     13          8           0        2.890263   -7.290313    1.609579
     14          6           0        2.618024   -2.868620   -0.364251
     15          6           0        1.276918   -3.159930   -0.063321
     16          6           0        0.278909   -2.210171   -0.229235
     17          6           0        0.566532   -0.925353   -0.724829
     18          6           0        1.902925   -0.640789   -1.059794
     19          6           0        2.906160   -1.587302   -0.856797
     20         16           0        2.324796    0.883353   -1.876405
     21          6           0        1.098651    1.947245   -1.145472
     22          6           0        1.382251    3.299703   -1.017865
     23          6           0        0.401193    4.220568   -0.602496
     24          6           0        0.719254    5.670815   -0.512995
     25          6           0       -0.249860    6.620395    0.160466
     26          6           0       -0.276516    6.477682    1.702421
     27          6           0        1.018297    6.889365    2.422256
     28          6           0        1.300762    8.397844    2.416784
     29          6           0        2.572187    8.774957    3.188829
     30          6           0        2.849917   10.281709    3.199041
     31          7           0        1.854016    5.999393   -1.030862
     32          8           0        2.113572    7.388155   -0.900314
     33          6           0        3.316288    7.762096   -1.463397
     34          6           0        3.485219    9.255132   -1.288940
     35          8           0        4.093456    7.016249   -1.994534
     36          6           0       -0.868529    3.714559   -0.298998
     37          6           0       -1.147667    2.351876   -0.385123
     38          6           0       -0.173287    1.435664   -0.804994
     39          7           0       -0.447655    0.049756   -0.892153
     40          6           0       -1.822251   -0.374462   -0.830297
     41          6           0       -2.518594   -0.600114   -2.022502
     42          6           0       -3.845950   -1.011686   -1.993175
     43          6           0       -4.511548   -1.211982   -0.769079
     44          6           0       -5.935935   -1.648970   -0.747804
     45          6           0       -6.579538   -2.145575    0.527995
     46          6           0       -7.319994   -1.023862    1.292163
     47          6           0       -7.917298   -1.479248    2.633381
     48          6           0       -9.041151   -2.518841    2.521814
     49          6           0       -9.668509   -2.875801    3.876078
     50          6           0      -10.789784   -3.913987    3.767433
     51          7           0       -6.542378   -1.544802   -1.880040
     52          8           0       -7.887786   -1.973727   -1.778319
     53          6           0       -8.547764   -1.969839   -2.993151
     54          6           0       -9.976649   -2.404973   -2.760634
     55          8           0       -8.052530   -1.670390   -4.044591
     56          6           0       -3.802347   -0.982140    0.420548
     57          6           0       -2.472171   -0.563560    0.392019
     58          1           0       10.463978   -7.823292    0.685354
     59          1           0        8.857813   -7.552873    1.378317
     60          1           0       10.237859   -6.604446    1.949446
     61          1           0       10.440316   -5.536802   -0.335793
     62          1           0        9.068032   -6.474924   -0.900485
     63          1           0        7.601682   -5.347266    0.804225
     64          1           0        8.974530   -4.397994    1.356829
     65          1           0        9.209584   -3.435629   -0.978598
     66          1           0        7.774623   -4.312283   -1.466981
     67          1           0        7.944133   -2.119227    0.677464
     68          1           0        7.313623   -1.917910   -0.948291
     69          1           0        6.056785   -3.643182    1.263697
     70          1           0        5.519738   -2.057204    0.744948
     71          1           0        5.052346   -3.022748   -1.568650
     72          1           0        5.511310   -4.608615   -0.962980
     73          1           0        4.929403   -8.847177    1.863300
     74          1           0        5.710729   -8.065073    0.457043
     75          1           0        5.966406   -7.407915    2.076765
     76          1           0        1.024312   -4.143758    0.315249
     77          1           0       -0.741235   -2.474551    0.019345
     78          1           0        3.923614   -1.303792   -1.103502
     79          1           0        2.372213    3.664923   -1.268393
     80          1           0        0.000967    7.643747   -0.120684
     81          1           0       -1.255777    6.426322   -0.229308
     82          1           0       -0.511810    5.437500    1.957874
     83          1           0       -1.109784    7.085419    2.081326
     84          1           0        1.870994    6.354844    1.980979
     85          1           0        0.953370    6.547438    3.464766
     86          1           0        1.391719    8.755174    1.382649
     87          1           0        0.441416    8.928933    2.853948
     88          1           0        3.430707    8.246155    2.750829
     89          1           0        2.489594    8.412183    4.223252
     90          1           0        2.970956   10.671471    2.180140
     91          1           0        2.024654   10.834339    3.664880
     92          1           0        3.764420   10.517399    3.755072
     93          1           0        2.622415    9.791459   -1.696299
     94          1           0        4.395280    9.569618   -1.800944
     95          1           0        3.558404    9.506392   -0.225199
     96          1           0       -1.667919    4.375558    0.016995
     97          1           0       -2.140863    2.003635   -0.131050
     98          1           0       -2.006690   -0.454138   -2.968728
     99          1           0       -4.384855   -1.186945   -2.917389
    100          1           0       -5.817205   -2.594198    1.173784
    101          1           0       -7.285297   -2.937203    0.265898
    102          1           0       -8.113472   -0.626250    0.647320
    103          1           0       -6.625549   -0.193342    1.474243
    104          1           0       -7.115404   -1.877116    3.273381
    105          1           0       -8.306566   -0.592848    3.153662
    106          1           0       -8.661049   -3.437793    2.053804
    107          1           0       -9.823193   -2.135158    1.849375
    108          1           0       -8.885227   -3.251900    4.549492
    109          1           0      -10.059057   -1.961723    4.345464
    110          1           0      -10.421214   -4.852540    3.335375
    111          1           0      -11.604163   -3.552842    3.127254
    112          1           0      -11.216755   -4.145434    4.749743
    113          1           0      -10.003623   -3.400249   -2.305182
    114          1           0      -10.502056   -2.420863   -3.715951
    115          1           0      -10.477332   -1.714738   -2.073625
    116          1           0       -4.283277   -1.117511    1.383323
    117          1           0       -1.934826   -0.385154    1.318823
 ---------------------------------------------------------------------

A-02

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0       -4.723809   -6.063769    0.577153
      2          6           0       -5.035479   -4.933671   -0.409215
      3          6           0       -4.852478   -3.539114    0.202253
      4          6           0       -5.175241   -2.406741   -0.796364
      5          6           0       -4.998658   -1.029239   -0.194544
      6          7           0       -5.909182   -0.405829    0.474659
      7          8           0       -7.098416   -1.179347    0.555751
      8          6           0       -8.132626   -0.514674    1.176669
      9          6           0       -9.324500   -1.444126    1.246776
     10          8           0       -8.084623    0.612834    1.588965
     11          6           0       -3.710542   -0.301911   -0.320347
     12          6           0       -3.597180    1.041514    0.076391
     13          6           0       -2.390289    1.720102   -0.011770
     14          6           0       -1.235304    1.097929   -0.520967
     15          6           0       -1.354294   -0.236601   -0.951445
     16          6           0       -2.560020   -0.924460   -0.827033
     17         16           0       -0.000037   -1.029813   -1.793319
     18          6           0        1.354196   -0.236571   -0.951440
     19          6           0        2.559943   -0.924391   -0.827016
     20          6           0        3.710434   -0.301800   -0.320309
     21          6           0        4.998568   -1.029090   -0.194489
     22          6           0        5.175341   -2.406400   -0.796694
     23          6           0        4.852749   -3.539107    0.201598
     24          6           0        5.035970   -4.933458   -0.410275
     25          6           0        4.724460   -6.063890    0.575761
     26          7           0        5.908955   -0.405802    0.475011
     27          8           0        7.098213   -1.179287    0.556072
     28          6           0        8.132342   -0.514675    1.177198
     29          6           0        9.324283   -1.444050    1.247156
     30          8           0        8.084242    0.612751    1.589704
     31          6           0        3.597029    1.041622    0.076424
     32          6           0        2.390114    1.720170   -0.011749
     33          6           0        1.235167    1.097954   -0.520963
     34          7           0       -0.000070    1.784293   -0.603060
     35          6           0       -0.000045    3.216939   -0.448973
     36          6           0        0.000130    3.818128    0.810952
     37          6           0        0.000171    5.209080    0.940294
     38          6           0        0.000051    6.011360   -0.208618
     39          8           0        0.000084    7.372150   -0.202501
     40          6           0        0.000237    8.043451    1.049597
     41          6           0       -0.000099    5.408813   -1.476689
     42          6           0       -0.000141    4.025396   -1.592693
     43          1           0       -4.864426   -7.046927    0.114080
     44          1           0       -5.376497   -6.012928    1.457156
     45          1           0       -3.687141   -6.006899    0.930838
     46          1           0       -6.067800   -5.036450   -0.772301
     47          1           0       -4.390317   -5.030755   -1.294090
     48          1           0       -5.502596   -3.430891    1.079421
     49          1           0       -3.821553   -3.429343    0.565480
     50          1           0       -6.212209   -2.509131   -1.127855
     51          1           0       -4.544111   -2.503690   -1.685690
     52          1           0       -9.604848   -1.784712    0.244764
     53          1           0       -9.079264   -2.331703    1.839590
     54          1           0      -10.160253   -0.914789    1.705527
     55          1           0       -4.470911    1.549339    0.468630
     56          1           0       -2.343522    2.752826    0.310029
     57          1           0       -2.585257   -1.960537   -1.147136
     58          1           0        2.585225   -1.960468   -1.147115
     59          1           0        6.212327   -2.508547   -1.128212
     60          1           0        4.544224   -2.503183   -1.686048
     61          1           0        3.821805   -3.429603    0.564851
     62          1           0        5.502843   -3.431037    1.078801
     63          1           0        4.390834   -5.030384   -1.295186
     64          1           0        6.068311   -5.035974   -0.773377
     65          1           0        4.865234   -7.046891    0.112404
     66          1           0        5.377128   -6.013205    1.455788
     67          1           0        3.687778   -6.007282    0.929449
     68          1           0        9.605292   -1.783567    0.244961
     69          1           0       10.159696   -0.915036    1.706898
     70          1           0        9.078830   -2.332268    1.838910
     71          1           0        4.470740    1.549476    0.468671
     72          1           0        2.343296    2.752895    0.310048
     73          1           0        0.000232    3.195404    1.701132
     74          1           0        0.000299    5.649444    1.930453
     75          1           0        0.000237    9.109240    0.815728
     76          1           0       -0.895052    7.800496    1.636409
     77          1           0        0.895644    7.800454    1.636213
     78          1           0       -0.000181    6.047422   -2.354111
     79          1           0       -0.000256    3.556437   -2.571980
 ---------------------------------------------------------------------

G-01

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0       -0.867394    9.598191    2.433490
      2          6           0       -0.805658    8.816059    1.117603
      3          6           0       -0.687107    7.300242    1.321924
      4          6           0       -0.625999    6.509849    0.008372
      5          6           0       -0.506981    4.994718    0.217306
      6          6           0       -0.450032    4.226540   -1.113357
      7          7           0       -0.336004    2.775972   -0.977634
      8          6           0       -1.481855    1.978174   -0.847602
      9          6           0       -2.780135    2.494876   -0.709418
     10          6           0       -3.887107    1.657426   -0.613909
     11          6           0       -3.747426    0.262183   -0.639797
     12          6           0       -4.930792   -0.625956   -0.525866
     13          6           0       -4.806827   -2.116208   -0.760003
     14          6           0       -4.563904   -2.902482    0.548172
     15          6           0       -4.488572   -4.419423    0.344031
     16          6           0       -4.321526   -5.219067    1.650202
     17          6           0       -3.920534   -6.632155    1.182597
     18          6           0       -3.143082   -6.421885   -0.151439
     19          6           0       -3.296531   -4.917952   -0.501456
     20          7           0       -6.027982   -0.029490   -0.199051
     21          8           0       -7.100913   -0.957325   -0.106536
     22          6           0       -8.314809   -0.355016    0.137237
     23          6           0       -9.367083   -1.434622    0.266920
     24          8           0       -8.496055    0.829242    0.229757
     25          6           0       -2.446612   -0.260311   -0.761767
     26          6           0       -1.349259    0.577156   -0.864571
     27          8           0       -0.116456   -0.028432   -1.017025
     28          6           0        1.007770    0.761808   -0.871324
     29          6           0        2.222761    0.105556   -0.775212
     30          6           0        3.427148    0.824089   -0.660547
     31          6           0        4.734930    0.130930   -0.553780
     32          6           0        4.841810   -1.361526   -0.780769
     33          6           0        4.714849   -2.169086    0.530626
     34          6           0        4.801734   -3.684990    0.322173
     35          6           0        4.611096   -4.508129    1.610589
     36          6           0        5.100911   -5.910478    1.217878
     37          6           0        6.322431   -5.651342    0.298272
     38          6           0        6.160224   -4.193102   -0.225585
     39          7           0        5.728796    0.891598   -0.237525
     40          8           0        6.933251    0.141622   -0.150086
     41          6           0        8.041077    0.925973    0.080327
     42          6           0        9.249182    0.023188    0.203474
     43          8           0        8.037414    2.124478    0.166797
     44          6           0        3.348003    2.224075   -0.634859
     45          6           0        2.123612    2.878916   -0.723674
     46          6           0        0.920766    2.166390   -0.854472
     47          1           0       -1.731126    9.292186    3.036461
     48          1           0        0.033002    9.430478    3.037157
     49          1           0       -0.951797   10.675936    2.254035
     50          1           0       -1.703295    9.031684    0.520741
     51          1           0        0.047884    9.168768    0.521327
     52          1           0       -1.540503    6.946512    1.919013
     53          1           0        0.211349    7.083387    1.918301
     54          1           0        0.226979    6.864999   -0.589208
     55          1           0       -1.524855    6.727581   -0.587837
     56          1           0        0.392116    4.768109    0.804731
     57          1           0       -1.357213    4.631264    0.808735
     58          1           0        0.397070    4.571751   -1.714866
     59          1           0       -1.343589    4.435311   -1.710482
     60          1           0       -2.937219    3.566084   -0.672216
     61          1           0       -4.877361    2.086073   -0.512687
     62          1           0       -5.733100   -2.471752   -1.220290
     63          1           0       -3.999342   -2.308146   -1.472242
     64          1           0       -3.634582   -2.554691    1.021243
     65          1           0       -5.375434   -2.667231    1.247612
     66          1           0       -5.420741   -4.751548   -0.141239
     67          1           0       -5.222993   -5.212822    2.273735
     68          1           0       -3.513184   -4.770249    2.245422
     69          1           0       -3.329486   -7.166770    1.933589
     70          1           0       -4.819916   -7.233454    1.003634
     71          1           0       -2.087825   -6.698861   -0.056245
     72          1           0       -3.559206   -7.053278   -0.944110
     73          1           0       -2.393654   -4.366830   -0.201254
     74          1           0       -3.430025   -4.750397   -1.575703
     75          1           0       -9.137499   -2.087674    1.115607
     76          1           0       -9.389792   -2.058949   -0.632101
     77          1           0      -10.339852   -0.965242    0.417124
     78          1           0       -2.254327   -1.326812   -0.779634
     79          1           0        2.198568   -0.977849   -0.793226
     80          1           0        4.071493   -1.681906   -1.489934
     81          1           0        5.810006   -1.571320   -1.241608
     82          1           0        5.508609   -1.849702    1.218508
     83          1           0        3.762374   -1.921646    1.018398
     84          1           0        4.009873   -3.984392   -0.383216
     85          1           0        5.244996   -4.093435    2.408159
     86          1           0        3.577687   -4.495715    1.976324
     87          1           0        4.311176   -6.428997    0.658946
     88          1           0        5.345950   -6.538194    2.081396
     89          1           0        7.257154   -5.751651    0.861208
     90          1           0        6.371932   -6.379255   -0.518387
     91          1           0        6.212354   -4.136199   -1.318028
     92          1           0        6.968530   -3.557874    0.160328
     93          1           0       10.137657    0.638024    0.350980
     94          1           0        9.127815   -0.659660    1.051057
     95          1           0        9.365060   -0.587799   -0.697583
     96          1           0        4.260000    2.801737   -0.539165
     97          1           0        2.112209    3.961523   -0.686989
 ---------------------------------------------------------------------

G-02

---------------------------------------------------------------------
 Center     Atomic      Atomic             Coordinates (Angstroms)
 Number     Number       Type             X           Y           Z
 ---------------------------------------------------------------------
      1          6           0       10.185154   -3.676892    1.019457
      2          6           0        9.115491   -2.607548    1.051083
      3          8           0        9.230308   -1.497973    1.496821
      4          8           0        7.972382   -3.120707    0.477542
      5          7           0        6.901952   -2.192615    0.449081
      6          6           0        5.841976   -2.701857   -0.079259
      7          6           0        5.719350   -4.107639   -0.613347
      8          6           0        4.672009   -1.790895   -0.144362
      9          6           0        4.736731   -0.483461    0.365882
     10          6           0        3.637051    0.361333    0.320622
     11          6           0        2.422178   -0.049079   -0.259301
     12          6           0        2.366558   -1.345251   -0.804144
     13          6           0        3.461490   -2.203232   -0.720265
     14         16           0        0.939314   -1.864480   -1.734544
     15          6           0       -0.313967   -0.966719   -0.842618
     16          6           0       -1.605088   -1.488132   -0.791443
     17          6           0       -2.670100   -0.752332   -0.251518
     18          6           0       -4.048456   -1.300334   -0.228398
     19          6           0       -4.283863   -2.744723   -0.595339
     20          7           0       -4.963238   -0.458981    0.114835
     21          8           0       -6.252417   -1.044787    0.081129
     22          6           0       -7.206454   -0.263238    0.693071
     23          8           0       -6.968816    0.741501    1.317077
     24          6           0       -8.566811   -0.843516    0.494515
     25          6           0       -8.818213   -1.943628   -0.338110
     26          6           0      -10.118300   -2.425936   -0.480358
     27          6           0      -11.171861   -1.817210    0.205523
     28          6           0      -10.924991   -0.719539    1.034263
     29          6           0       -9.628404   -0.232954    1.177197
     30          6           0       -2.385940    0.525459    0.258271
     31          6           0       -1.094178    1.032023    0.248446
     32          6           0       -0.024355    0.297598   -0.296267
     33          7           0        1.295933    0.807442   -0.302059
     34          6           0        1.488671    2.201360    0.013368
     35          6           0        1.531011    2.639180    1.365063
     36          6           0        1.715678    3.971444    1.653156
     37          6           0        1.866867    4.931642    0.615826
     38          6           0        2.058989    6.313484    0.881902
     39          6           0        2.201761    7.214896   -0.148902
     40          6           0        2.158937    6.775798   -1.495101
     41          6           0        1.974146    5.443129   -1.786625
     42          6           0        1.823638    4.487750   -0.746116
     43          6           0        1.631698    3.105938   -1.014009
     44          1           0       11.093492   -3.282907    1.476388
     45          1           0        9.851891   -4.566606    1.563803
     46          1           0       10.390795   -3.979874   -0.012523
     47          1           0        4.908014   -4.639451   -0.103658
     48          1           0        5.476700   -4.089248   -1.682172
     49          1           0        6.644727   -4.663228   -0.475190
     50          1           0        5.661682   -0.138222    0.813562
     51          1           0        3.723803    1.357624    0.736064
     52          1           0        3.358117   -3.199435   -1.137033
     53          1           0       -1.771663   -2.474212   -1.212284
     54          1           0       -4.172028   -2.889217   -1.677198
     55          1           0       -3.551623   -3.389515   -0.099702
     56          1           0       -5.285453   -3.062160   -0.309384
     57          1           0       -8.000931   -2.411150   -0.875392
     58          1           0      -10.309894   -3.276721   -1.128477
     59          1           0      -12.184058   -2.196627    0.092891
     60          1           0      -11.743491   -0.243668    1.567202
     61          1           0       -9.413370    0.620103    1.812168
     62          1           0       -3.191948    1.115114    0.680122
     63          1           0       -0.912875    2.014405    0.666468
     64          1           0        1.415863    1.908691    2.160419
     65          1           0        1.748091    4.306164    2.687004
     66          1           0        2.091458    6.648147    1.915903
     67          1           0        2.348210    8.269585    0.066945
     68          1           0        2.272923    7.497810   -2.298863
     69          1           0        1.940827    5.103188   -2.818757
     70          1           0        1.597135    2.756402   -2.042118
 ---------------------------------------------------------------------

Synthetic Routes and NMR

F-01

Schema S2 Synthesis root of F-01

For the first step of the synthesis, the starting 4-methylbenzophenone derivative is dissolved in ethanol, followed by the addition of hydroxylamine hydrochloride (NH2OH•HCl). The reaction mixture is heated to 80°C and maintained at this temperature until the reaction reaches completion. After cooling to room temperature, the intermediate amine product is isolated and purified.

In the second step, the purified amine intermediate is dissolved in dichloromethane (DCM). Pyridine is added as a base to the solution. The acyl chloride is then added dropwise to the reaction mixture, which is stirred at room temperature. Upon completion of the reaction, standard workup procedures are performed, and the final N-acylated product is purified using appropriate methods.

Throughout both steps, reaction progress should be carefully monitored using appropriate analytical methods. Standard inert atmosphere techniques may be employed if the reagents are moisture sensitive. Care should be taken during the acyl chloride addition to control the exothermic nature of the reaction.

F-02

Schema S3 Synthesis root of F-02

The synthesis begins with 2-acetonaphthone dissolved in ethanol. To this solution, hydroxylamine hydrochloride (NH2OH•HCl) is added, and the reaction mixture is heated to 80°C. The reaction is maintained at this temperature until completion, yielding the corresponding oxime intermediate. After cooling to room temperature, the oxime product is isolated and purified.

For the second step, the purified oxime intermediate is dissolved in dichloromethane (DCM). Pyridine is added to the solution as a base. The acetyl chloride is then carefully added dropwise to the reaction mixture at room temperature. The reaction is stirred until completion, followed by appropriate workup procedures. The final N-acetylated oxime product is then isolated and purified using suitable methods.

Throughout the synthesis, the reaction progress should be monitored using appropriate analytical techniques. The addition of acetyl chloride should be performed carefully to control the exothermic nature of the reaction.

A-01

Schema S4 Synthesis root of A-01

The synthesis begins with phenothiazine, which undergoes an aryl iodide coupling reaction. The phenothiazine is combined with 4-iodotoluene in the presence of copper(I) chloride and potassium carbonate. The reaction mixture is heated to reflux in N-methyl-2-pyrrolidone for the cross-coupling reaction to proceed, yielding the N-arylated phenothiazine intermediate.

In the second step, the N-arylated phenothiazine intermediate undergoes a Friedel-Crafts acylation. The substrate is treated with hexanoyl chloride under appropriate conditions to introduce two hexanoyl groups at the 3 and 7 positions of the phenothiazine core, producing the diketone intermediate.

The third step involves the conversion of both ketone groups to oximes. The diketone intermediate is dissolved in ethanol, and hydroxylamine hydrochloride (NH2OH•HCl) is added. The reaction mixture is heated to 80°C until the conversion is complete, forming the dioxime product.

In the final step, both oxime groups are acetylated. The dioxime intermediate is dissolved in dichloromethane (DCM), and triethylamine (TEA) is added as a base. Acetyl chloride is then carefully added dropwise at room temperature. The reaction is stirred until completion, yielding the final bis-N-acetylated oxime product.

Each step requires appropriate workup and purification procedures. The reaction progress should be monitored throughout using suitable analytical methods. Care should be taken during the addition of acetyl chloride in the final step due to the exothermic nature of the reaction.

A-02

Schema S5 Synthesis root of A-02

The synthesis starts with phenothiazine and 4-iodofluorobenzene. These compounds are combined with copper(I) chloride and potassium carbonate as catalysts, and the reaction mixture is heated at reflux in N-methyl-2-pyrrolidone. This Ullmann-type coupling reaction yields the N-(4-fluorophenyl)phenothiazine intermediate.

In the second step, the fluorinated phenothiazine intermediate undergoes a Friedel-Crafts acylation. The substrate is dissolved in dichloromethane (DCM), and aluminum chloride is added as a Lewis acid catalyst. Butyryl chloride is then carefully added to the reaction mixture at 0°C. After warming to room temperature, the reaction proceeds to form the dibutyryl product with acylation occurring at the 3 and 7 positions of the phenothiazine core.

The third step involves the conversion of both ketone groups to oximes. The diketone intermediate is dissolved in ethanol, and a mixture of hydroxylamine hydrochloride (NH2OH•HCl) and sodium acetate trihydrate is added. The reaction mixture is heated to 80°C and maintained at this temperature until the conversion to the dioxime is complete.

In the final step, both oxime groups are acetylated. The dioxime intermediate is dissolved in dichloromethane (DCM), and triethylamine (TEA) is added as a base. Acetyl chloride is then carefully added dropwise at room temperature. The reaction is stirred until completion to yield the final bis-N-acetylated oxime product.

Throughout the synthesis, each step requires appropriate workup and purification procedures. Reaction progress should be monitored using suitable analytical methods such as TLC or NMR spectroscopy. Special attention should be paid to maintaining anhydrous conditions during the Friedel-Crafts acylation and controlling the temperature during the addition of reagents.

G-01

Schema S6 Synthesis root of G-01

The synthesis begins with phenoxathiin as the starting material. In the first step, the phenoxathiin undergoes a Friedel-Crafts acylation reaction. The substrate is dissolved in dichloromethane (DCM), and aluminum chloride is added as a Lewis acid catalyst. Cyclopentylacetyl chloride is then carefully added to the reaction mixture at 0°C. After warming to room temperature, the reaction proceeds to form the diacylated product with acylation occurring at the 2 and 8 positions of the phenoxathiin core, introducing two cyclopentylacetyl groups.

In the second step, both ketone groups are converted to oximes. The diketone intermediate is dissolved in ethanol, and hydroxylamine hydrochloride (NH2OH•HCl) is added. The reaction mixture is heated to reflux temperature and maintained until the conversion to the dioxime is complete. Upon cooling, the dioxime product is isolated and purified.

The final step involves the acetylation of both oxime groups. The dioxime intermediate is dissolved in dichloromethane (DCM), and acetyl chloride is added carefully at room temperature. The reaction is stirred until completion to yield the final bis-N-acetylated oxime product.

Throughout each step of the synthesis, appropriate workup and purification procedures should be performed. The reaction progress should be monitored using suitable analytical methods such as TLC or NMR spectroscopy. Particular attention should be paid to maintaining anhydrous conditions during the Friedel-Crafts acylation step and controlling the temperature during the addition of reagents.

G-02

Schema S7 Synthesis root of G-02

The synthesis begins with phenoxazine as the starting material. In the first step, the N-alkylation of phenoxazine is performed using 1-bromohexane. The phenoxazine is dissolved in DMSO, and potassium hydroxide is added as a base. The reaction mixture is heated to 70°C, and 1-bromohexane is added. The reaction is maintained at this temperature until the N-alkylated phenoxazine product is formed.

In the second step, the N-alkylated phenoxazine undergoes a Friedel-Crafts acylation. The substrate is dissolved in an appropriate solvent, and aluminum chloride is added as a Lewis acid catalyst. Cyclopentylacetyl chloride is then carefully added to the reaction mixture. The reaction proceeds to form the diacylated product with acylation occurring at the 2 and 8 positions of the phenoxazine core, introducing two cyclopentylacetyl groups.

The third step involves the conversion of both ketone groups to oximes. The diketone intermediate is dissolved in ethanol, and hydroxylamine hydrochloride (NH2OH•HCl) is added. The reaction mixture is heated until the conversion to the dioxime is complete. Upon cooling, the dioxime product is isolated and purified.

In the final step, both oxime groups are acetylated. The dioxime intermediate is dissolved in dichloromethane (DCM), and pyridine is added as a base. Acetyl chloride is then carefully added dropwise at room temperature. The reaction is stirred until completion to yield the final bis-N-acetylated oxime product.

Throughout the synthesis, each step requires appropriate workup and purification procedures. The reaction progress should be monitored using suitable analytical methods such as TLC or NMR spectroscopy. Particular attention should be paid to maintaining anhydrous conditions during the Friedel-Crafts acylation step and controlling the temperature during the addition of reagents.

NMR Spectrum

F-01

Figure S6 NMR spectra of F-01

F-02

Figure S7 NMR spectra of F-02

A-01

Figure S8 NMR Spectra of A-01

A-02

Figure S9 NMR Spectra of A-02

G-01

Figure S10 NMR Spectra of G-01

G-02

Figure S11 NMR Spectra of G-02

References

X. Wu, S. Gong, Z. Chen, J. Hou, Q. Liao, Y. Xiong, Z. Li, and H. Tang, Dyes Pigments, 2022, 205, 110556.

Y. H. Wu, B. Graff, J. Lalevée and Y. C. Chen, Eur. Polym. J., 2024, 217, 113300.

F. Hammoud, A. Hijazi, M. Schmitt, F. Dumur and J. Lalevée, Eur. Polym. J., 2023, 188, 111901.

W. J. Lee, H. S. Kwak, D. Lee, C. Oh, E. Yum, Y. An, M. D. Halls, and C. Lee., Chem. Mater., 2022, 34, 116–127.

Z. J. Baum, X. Yu, P. Y. Ayala, Y. Zhao, S. P. Watkins, and Q. Zhou, J. Chem Inf. Model., 2021, 61, 3197–3212.

V. Bagal, R. Aggarwal, P. K. Vinod and U. Deva Priyakumar, J. Chem. Inf. Model, 2022, 62, 2064.

S. Ishida, T. Aasawat, M. Sumita, M. Katouda, T. Yoshizawa, K. Yoshizoe, K. Tsuda, and K. Terayama, Wiley Interdiscip. Rev. Comput. Mol. Sci., 2023, 13, e1680.

P. Ertl and A. Schuffenhauer, J. Cheminform., 2009, 1, 1–11.

G. Skoraczyński, M. Kitlas, B. Miasojedow and A. Gambin, J. Cheminform., 2023, 15, 1–9.

O. O. Grygorenko, D. S. Radchenko, I. Dziuba, A. Chuprina, K. E. Gubina, and Y. S. Moroz, iScience, 2020, 23.

S. Liu, N. Giacoletto, M. Schmitt, M. Nechab, B. Graff, F. Morlet-Savary, P. Xiao, F. Dumur, and J. Lalevee, Macromolecules, 2022, 55, 2475–2485.

R. Zhou, H. Pan, D. Wan, J. P. Malval and M. Jin, Prog. Org. Coat., 2021, 157.

F. Hammoud, Z. Lee, B. Graff, A. Hijazi, J. Lalevée, and Y. Chen, J. Polym. Sci., 2021, 59, 1711–1723.

W. Wang, M. Jin, H. Pan and D. Wan, Dyes Pigments, 2021, 192.

W. Wang, M. Jin, H. Pan and D. Wan, Prog. Org. Coat., 2021, 151, 106019.

S. Liu, B. Graff, P. Xiao, F. Dumur and J. Lalevée, Macromol. Rapid Commun., 2021, 42.

M. Rahal, H. Bidotti, S. Duval, B. Graff, T. Hamieh, J. Toufaily, F. Dumur, J. Lalevée, Eur. Polym. J., 2022, 177.

Z. Li, X. Zou, G. Zhu, X. Liu and R. Liu, ACS Appl. Mater. Interfaces, 2018, 10, 16113–16123.

S. Kim, J. Chen, T. Cheng, A. Gindulyte, J. He, S. He, Q. Li, B. A. Shoemaker, P. A. Thiessen, B. Yu, L. Zaslavsky, J. Zhang, Nucleic Acids Res., 2023, 51, D1373–D1380.

M. Ibrahim-Ouali and F. Dumur, Eur. Polym. J., 2021, 158.

F. Hammoud, N. Giacoletto, G. Noirbent, B. Graff, A. Hijazi, M. Nechab, D. Gigmes, F. Dumur, and J. Lalevée, Mater. Chem. Front., 2021, 5, 8361–8370.

Y. Ding, S. Jiang, Y. Gao, J. Nie, H. Du, and F. Sun, Macromolecules, 2020, 53, 5701.

Z. H. Lee,  S. Yen, F. Hammoud, A. Hijazi, B. Graff, J. Lalevée, and Y. Chen, Polymers (Basel), 2022, 14, 5261.

Z. Liu and F. Dumur, Eur. Polym. J., 2022, 177.

X. Guo, W. Wang, D. Wan and M. Jin, Eur. Polym. J., 2021, 156, 110617.

W. Qiu, P. Hu, J. Zhu, R. Liu, Z. Li, Z. Hu, Q. Chen, K. Dietliker, and R. Liska, ChemPhotoChem, 2019, 3, 1090–1094.

F. Hammoud, N. Giacoletto, M. Nechab, B. Graff, A. Hijazi, F. Dumur, and J. Lalevée, Macromol. Mater. Eng., 2022, 307, 2200082.

Y. Zhang, F. Morlet-Savary, M. Schmitt, B. Graff, A. Rico, M. Ibrahim-Ouali, F. Dumur, and J. Lalevée, Dyes Pigments, 2023, 215, 111202.

M. J. Frisch et al., Gaussian 16, Revision A.03, Gaussian, Inc., Wallingford, CT, USA, 2016, Preprint.

G. A. Landrum, RDKit: Open-source cheminformatics, 2010. Preprint.

S. Riniker and G. A. Landrum, J. Chem. Inform. Model., 2015, 55, 2562.

T. Halgren, J. Comput. Chem., 1996, 17, 5/6.

D. E. Rumelhart, G. E. Hinton and R. J. Williams, Nature, 1986, 323, 533–536.

C. Liu, Y. Sun, R. Davis, S. T. Cardona and P. Hu, J. Cheminform., 2023, 15, 1–14.

A. Radford, J. Wu, R. Child, D. Luan, D. Amodei, and I. Sutskever, OpenAI Blog, 2019, 1, 9.

A. Paszke, S. Gross, F. Massa, A. Lerer, J. Bradbury, G. Chanan, T. Killeen et al., Adv. Neural Inform. Process. Systems, 2019, 32.

H. L. Morgan, J. Chem. Doc., 1965, 5, 107–113.

J. Gasteiger and M. Marsili, Tetrahedron, 1980, 36, 3219–3228.

E. Mazuz, G. Shtar, B. Shapira and L. Rokach, Sci. Rep., 2023, 13, 8799.

D. Weininger, J. Chem. Inf. Comput. Sci., 1988, 28, 31–36.

V. I. Levenshtein, Sov. Phys. Dokl., 1966, 10, 707–710.

F. Pedregosa, M. Eickenberg, P. Ciuciu, B. Thirion, and A. Gramfort, J. Mach. Learn. Res., 2011, 12, 2825–2830.

M. C. Rusu, C. Block, G. Van Assche and B. Van Mele, J. Therm. Anal. Calorim., 2012, 110, 287–294.

J. Bachmann, E. Gleis, S. Schmölzer, G. Fruhmann and O. Hinrichsen, Anal. Chim. Acta, 2021, 1153, 338268.